134 Pancharatna Char Rasta G.I.D.C.,Vapi.396195 Gujarat India

## Tel-Fax No. 91- 260 - 6618618, 09227788155,Fax No. 91- 260 - 6618624

Email: info@trivenichemical.com,Website:www.triveniinterchem.com

Technical Data Sheet

Material: Ammonium Bifluoride

General Information:

CAS No.: 1341-49-7

Formula: F2H5N

Synonyms: Ammonium hydrogen fluoride

Technical Data:

| Sr. No. | Test | Result |
| --- | --- | --- |
| 1. | Assay | 98.11% |
| 2. | Fluorine as F | 64.24% |
| 3. | Acidity as HF | 34.14% |
| 4. | Chloride as CL | 0.04% |

Characteristics:

Ammonium hydrogen fluoride is the inorganic compound with the formula NH4HF2 or NH4F·HF. It is produced from ammonia and hydrogen fluoride. This colourless salt is a glass-etchant and an intermediate in a once-contemplated route to hydrofluoric acid.

Applications:

It is used in Finishing agents, Intermediates, Plating agents and surface treating agents, Processing aids, not otherwise listed, Processing aids, specific to petroleum production, Solvents (for cleaning and degreasing) and as water treatment chemical.

Health & Safety Information:

Inhalation of dust may cause irritation of the respiratory system. Contact with dust irritates eyes.

Fire - Extinguish fire using agent suitable for type of surrounding fire. (Material itself does not burn or burns with difficulty.) Use water in flooding quantities as fog.

For full safety information please refer the Safety Data Sheet.